Part of the national titanium industry standards

| country | Standard code abbreviation |  |
| --- | --- | --- |
| China | GB | national standards |
|  | GB/T | National recommendation standard |
|  | YB | Department of Metallurgy Standard |
|  | YS/T | Non-ferrous metals industry standards |
|  | GJB | National military standards |
| America | ASTM | American Association of Testing and Materials Standards |
|  | ASME | The American Institute of Mechanical Engineers standards |
|  | AMS | American Technical Standards for Aerospace Materials |
|  | MIL-T MIL-STD | U. S. military standards |
| Russia | COCT | Former Soviet national standard |
|  | OCT | Former Soviet departmental standards |
| Japan | JISH | The Japanese (Titanium) industrial standard |
|  | JIS7505 | The Japanese titanium casting standard |
| France | NFL | The French Titanium Industry Standard |
| Germany | DIN | The German Titanium Industry Standard |
| Britain | BS | The UK Titanium Industry Standard |
| ISO | ISO | international standard |

Titanium and titanium alloy standards

1. Chinese Industrial Standards

1. National standards of China

GB / T2524-2007 titanium sponge

GB / T3620-2007 Titanium and titanium alloy brand and chemical composition

GB / T15073-1994, casting titanium and titanium alloy brand and chemical composition

GB / T3621-2007 Titanium and titanium alloy sheet

GB / T14845-1993 Titanium plate for plate heat exchanger

GB / T3622-1999 Titanium and titanium alloy bands and foils

GB / T3623-2007 Titanium and titanium alloy wire

GB / T3624-2007 Titanium and titanium alloy pipe material

GB / T3625-2007 Titanium and titanium alloy tubes for heat exchangers and condensers

GB / T2965-2007 Titanium and titanium alloy bars

GB / T16598-1996 Titanium and titanium alloy cake and ring

GB / T8546-1987 Titanium-stainless-steel composite plate

GB / T8547-1987 Titanium-steel composite plate

GB / T6614-1994 Titanium and titanium alloy castings

GB / T5168-1985 Method of two-phase titanium alloy

GB / T6611-2008 Titanium and titanium alloy terms

GB / T8755-2008 Titanium and titanium alloy term metallographic diagram

GB / T12769-2003 Ti-copper composite rod

GB / T13810-2007, titanium and titanium alloy materials for surgical implants

GB / T12417-1990

GB/T4698.1-4698.25-1996 Chemical analysis method for sponge titanium, titanium and titanium alloys

GB / T5193-2007 ultrasonic flaw detection method for titanium and titanium alloy processing products

GB/T12969.1-1991 Ultrasonic inspection method for titanium and titanium alloy pipes

GB/T12969.2-1991 Testing method of titanium and titanium alloy pipe

GB / T13149-1991 Titanium and titanium alloy meet the technical conditions of steel plate welding

GB / T6887-1986 Sintered titanium metal filter elements and materials

Packaging, marking, transportation and storage of GB / T8180-2007 titanium and titanium alloy processing products

GB / T6612-1986, important TA7 titanium alloy plate

GB / T6613-1986, important TC4 titanium alloy plate

GB / T1216-1992 TA5 titanium alloy welding technical conditions

2. National Military standards of China

GJB2218-1994 Specification for titanium and titanium alloy bars and forging blanks for aviation

GJB2219-1994 Specification for titanium and titanium alloy rods (wire) for fasteners

GJB2220-1994 Specification for titanium alloy cake and ring billet for aero engine

GJB2505-1995 Specification for titanium and titanium alloy plates and strip for aviation

GJB2744-1996 Specification for titanium and titanium alloy bars and free forgings and die forgings for aviation

GJB2896-1996 Specification for precision castings of titanium and titanium alloy melt mold

GJB2921-1997 Specification for TC4 titanium alloy plate for superplastic forming

GJB3763A-2004 titanium and titanium alloy heat treatment

GJB391-1987 TC4 titanium alloy forged cake material for aerospace industry

GJB493-1988 TC4 titanium alloy bar for aero-engine blades

GJB494-1988 TC11 titanium alloy bar for aero-engine blades

GJB495-1988 TA7-D titanium alloy bar

GJB943 TA5-A titanium alloy forgings for GJB943-1900 submarine

GJB944-1900 TA5-A titanium alloy sheet

GJB1169-1991 Specification for titanium alloy ring material for aerospace use

GJB1205-1991 TB2-1 titanium alloy rivet technical condition

GJB1538-1992 Specification for TC4 titanium alloy bars for aircraft structure parts

2. USASI

1. American Association of Testing and Materials Standards

ASTM B229-2001 titanium sponge

ASTM B265-2005 Titanium and titanium alloy belt, thin sheet and plate

ASTM B337-1995 Titanium and titanium alloy seamless pipe and welded pipe (has been replaced by B861-2002 titanium and titanium alloy seamless pipe, B862-2002 titanium and titanium alloy welded pipe)

ASTM B338-2005 A for titanium and titanium alloy condensers and heat exchangers

Seamless pipes and welded pipes

ASTM B348-2005, titanium and titanium alloy rods and blanks

ASTM B363-2004 Non-alloy titanium and titanium alloy seamless and welded pipe fittings

ASTM B367-2004 Titanium and titanium alloy castings

ASTM B861-2002 Titanium and titanium alloy seamless pipe

ASTM B862-2002 Titanium and titanium alloy welded pipe

ASTM B381-2005 Titanium and titanium alloy forgings

Pure titanium material for ASTM F67-2000 surgical implants

ASTM F136-2002a-Ti-6Al-4 VELI-processing materials for surgical implants

ASTM F620-2002 α + β phase titanium alloy forgings for surgical implants

ASTM F1108-2002 Ti-6Al-4V casting for surgical implants

ASTM F1295-2001 Ti-6Al-7 Nb

ASTM F1341-1999 Pure titanium wire

Ti-6Al-4V for ASTM F1472-2002a surgical implants

ASTM F1713-1996 Processing materials for Ti-13 Nb-13 Zr for surgical implants

ASTM F1813-2001 Ti-12Mo-6 Zr-2Fe materials for surgical implants

ASTM F2063-2000 for medical devices and surgical implants

Shape memory alloy processing material

2. The American Institute of Mechanical Engineers standards

ASME Part VIII: Chapter I Pressure Vessel (Basic Rules)

American Technical Standards for Aerospace Materials

AMS 4900-2001 Titanium sheet, strip and plate (annealed state) (380 Mpa)

AMS4901-2002 Titanium sheet, strip and plate (annealed state) (485 Mpa)

AMS4902-2001 Titanium sheet, strip and plate (annealed state) (275 Mpa)

AMS4907-2001 Ultra-low clearance element grade Ti-6Al-4V alloy sheet,

Belt and plate (annealed state)

AMS4910-2003 Ti-5Al-2.5Sn alloy sheet, strip and medium plate (annealed state)

AMS4911-2003 Ti-6Al-4V thin plate, belt, and medium thick plate (annealed state)

AMS4921-2004 Titanium bars, forgings, and rings (annealed state) (485 Mpa)

AMS4924-2002 Ultra-low clearance element grade Ti-5Al-2.5Sn alloy rod,

Forgings and rings (annealed state)

AMS4926-2001 Ti-5Al-2.5Sn rod and ring piece (annealed state) (760 Mpa)

AMS4928-2001 Ti-6Al-4V alloy rods, forgings, and rings

(Annealed state) (825 Mpa)

AMS4941-2003 Titanium welded pipe

AMS4942-2001 Seamless titanium tube (annealed state) (275 Mpa)

AMS4930-2001 Ultra-low clearance element grade Ti-6Al-4V alloy bar,

Forgings and rings (annealed state)

AMS4951-2003 Industrial pure titanium welding wire

AMS4954-2003 Ti-6Al-4V alloy welding wire

AMS4965-2002 Ti-6Al-4V alloy rods, forgings, and rings

(Solid solution and stabilization treatment)

AMS4966-2003 Ti-5Al-2.5Sn forgings

AMS4967-2001 Heat able Ti-6Al-4V alloy rods and forgings

And ring (annealed state)

ASM4972-2003 Ti-8Al-1Mo-1V alloy rod and ring parts

(Solid solution and stabilization treatment)

ASM4973-2002 Ti-8Al-1Mo-1V titanium alloy forgings

(Solid solution and stabilization treatment)

ASM4975-2003 Ti-6Al-2 Sn-4 Zr-2Mo alloy rods and rings

(Solid solution and stabilization treatment)

ASM4983-2002 Ti-10V-2F-3Al forging (solid solution treatment and aging)

ASM4985-2003 Ti-6Al-4V alloy forgings cast by paraffin wax or graphite tamping method

ASM4991-2002 Ti-6Al-4V Alloy fine forging (annealed state)

ASM2380-2003 Quality titanium alloy approved and controlled

3. American military standards

MIL-T-9046-1999 Titanium and titanium alloy sheet, strip and sheet

MIL-T-9047-2005 Titanium and titanium alloy bars and forging

MIL-R-81588-1986 Titanium and titanium alloy round rods and wires

MIL-F-83142-2000 Titanium and Titanium alloy forging (premium grade)

MIL-T-46077 Ti-alloy weldable armor thick plate

MIL-T-13405 Titanium powder

MIL-T-46035-1989 High strength titanium alloy, deformed material

MIL-T-81556-1996 Titanium and titanium alloy of the round rod, rod,

Extrusion parts of the special shape surface

Heat treatment of MIL-T-81200 titanium and titanium alloy

3. BS

BS2TA1:1974 Plate and strip of industrial pure titanium (tensile strength 290-420 Mpa)

BS2TA2:1973 Plate and strip (tensile strength 390-540 Mpa)

BS2TA3:1973 industrial pure titanium rod and profile for machining

(Tensile strength of 390-540 Mpa)

BS2TA4:1973 Forging billet of industrial pure titanium (tensile strength 390-540 Mpa)

BS2TA5:1973 Forging billet of industrial pure titanium (tensile strength 390-540 Mpa)

BS2TA6:1973 Plate and strip (tensile strength 570-730 Mpa)

BS2TA7:1973 industrial pure titanium rod and profile for machining

(Tensile strength of 540-740 Mpa)

BS2TA8:1973 Forging billet of industrial pure titanium (tensile strength 540-740 Mpa)

BS2TA9:1973 forgings of industrial pure titanium (tensile strength 540-740 Mpa)

BS2TA10:1974 titanium-aluminum-vanadium alloy

(Tensile strength 960-1270 Mpa)

BS2TA11:1974 Titanium-aluminum-vanadium alloy bar and profiles for machining

(Tensile strength of 900-1160 Mpa)

BS2TA12:1974 titanium-aluminum-vanadium alloy forging billet (tensile strength: 900-1160 Mpa)

BS2TA13:1974 Titanium-aluminum-vanadium alloy forging (Tensile strength: 900-1160 Mpa)

BS2TA21: Plate and strip of 1973 titanium-copper alloy (tensile strength 540-770 Mpa)

BS2TA22:1973 titanium-copper alloy bar and profiles for machining

(Tensile strength of 540-770 Mpa)

BS2TA23:1973 titanium-copper alloy (tensile strength 540-770 Mpa)

BS2TA24:1973 titanium-copper alloy forging (tensile strength 540-770 Mpa)

BS2TA28:1974, titanium-aluminum-vanadium alloy forging billet and wire

(Tensile strength 1100-1300 Mpa)

BSTA38:1993 machining of titanium-aluminum-molybdenum-tin-silicon-carbon alloy bar

(Tensile strength of 1250-1420 Mpa)

BSTA39:1993 titanium-aluminum-molybdenum-tin-silicon-carbon alloy forging billet

(Tensile strength of 1250-1420 Mpa)

BSTA40:1993 machining of titanium-aluminum-molybdenum-tin-silicon-carbon alloy bar

(Tensile strength 1250-1375 Mpa)

BSTA41:1993 titanium-aluminum-molybdenum-tin-silicon-carbon alloy forging billet

(Tensile strength 1250-1375 Mpa)

BSTA42:1993 titanium-aluminum-molybdenum-tin-silicon-carbon alloy forgings

(Tensile strength 1250-1375 Mpa)

BSTA45:1993 machining titanium-aluminum-molybdenum-tin-silicon alloy bar and profiles

(Tensile strength 1100-1280 Mpa)

BSTA46:1993 machining titanium-aluminum-molybdenum-tin-silicon alloy bar and profiles

(Tensile strength 1050-1220 Mpa)

BSTA47:1993 titanium-aluminum-molybdenum-tin-silicon alloy forging billet

(Tensile strength 1050-1220 Mpa)

BSTA48:1993 titanium-aluminum-molybdenum-tin-silicon alloy forging billet

(Tensile strength 1050-1220 Mpa)

BSTA49:1993 machining titanium-aluminum-molybdenum-tin-silicon alloy bar and profiles

(Tensile strength 1000-1200 Mpa)

BSTA50:1993 titanium-aluminum-molybdenum-tin-silicon alloy forging billet

(Tensile strength 1000-1200 Mpa)

BSTA51:1993 titanium-aluminum-molybdenum-tin-silicon alloy forgings

(Tensile strength 1000-1200 Mpa)

BSTA52:1993 Plate and strip of titanium-copper alloy (tensile strength 690-920 Mpa)

BSTA56:1993 Ti-aluminum-vanadium alloy thick plate (tensile strength 895-1150 Mpa)

BSTA57:1993 Ti-aluminum-Mo-tin-silicon thick plate (tensile strength 1030-1220 Mpa)

BSTA58:1993 titanium-copper alloy thick plate (tensile strength 520-640 Mpa)

BSTA100:1973 Inspection and experimental methods of deformed titanium and titanium alloys

BS5500:1997 flame welding pressure vessel

CP3003 Pressure vessel lining and chemical equipment

4. The Russian standard

Γ OCT17746-79 titanium sponge

Γ OCT19807-91 Deformed titanium and titanium alloy brand

Γ OCT22178-90 Titanium and titanium alloy thin sheet

Γ OCT23755-87 Titanium and titanium alloy thick plate

Γ OCT21945-82 hot-rolled seamless titanium pipe

Γ OCT22897-86 cold-rolled seamless titanium pipe

Γ OCT24890-81 Welded titanium pipe

Γ OCT26492-85 Titanium and titanium alloy rolled rods

Γ OCT27265-87, instructions for titanium and titanium alloy filling wire

5. Japanese standard

JISH2151-1983 titanium sponge

JISH4600-1993 Titanium and titanium alloy plates and strip

JISH4630-1994 Titanium and titanium alloy seamless pipe

JISH4631-1994 Titanium and titanium alloy heat exchanger tube

JISH4635-1994 Titanium and titanium alloy welded pipe

JISH4650-2000 titanium and titanium alloy rods

JISH4657-1998 Titanium and titanium alloy forgings

JISH4670-1993 Titanium and titanium alloy wire

JIS7505 Titanium castings

6. German standards

DIN17850-1990 Chemical composition of industrial pure titanium pressure processing material

DIN17851-1990, the chemical composition of the titanium alloy pressure processing material

DIN17860-1990 Titanium and titanium alloy plate and strip

DIN17861-1990 titanium and titanium alloy seamless tubes

DIN17862-1990 Titanium and titanium alloy rods

DIN17863-1973 Titanium and titanium alloy wire

DIN17864-1993 Titanium and titanium alloy forgings

DIN17865-1990 cast titanium

DIN17866-1990 titanium and titanium alloy welded pipe

DIN1737T1-1984 Chemical composition and technical conditions of titanium and titanium-palladium alloy filling materials

DIN1737T2-1988 Titanium and titanium palladium alloy filling material fully welded metal test block, sample, mechanics and process properties

DIN931 Outer hexagon bolt half thread

DIN933 Full threads of the external hexagon bolt

DIN931 Outer hexagon nut

DIN125 Ordinary gaskets

DIN127 Spring gasket

7. French standards

NFL 21-110 1975 Pure titanium T40 forging bar billet

NFL 21-270 1981 TA6V vet rod

NFL 14-601 1984 TA6V for forging bars

NFL 14-602 1984 TA6V forgings

NFL 14-603 1984 TA6V forging rod billet

NFL 14-604 1984 TA6V forgings

NFL 14-611 1984 TA6VZr5D bar blank

NFL 14-612 1984 TA6VZr5D forgings

VIII. ISO International Standard (Standard for Titanium for Surgical Implants)

ISO5832-2-1999 Pure titanium

ISO5832-3-1996 Ti-6Al-4V processing material

ISO5832-11-1994 Ti-6Al-7 Nb processing material